Miller Environmental Corp. Description and Specifications for Double Sided Butyl Tape

Typical application is for non-pressure water tight seaming in the field for our breakout barrier (MBE40M), pond liners, etc.

Butyl tape is a double-sided aggressive reinforced black butyl rubber tape used to join panels of polyethylene and polypropylene together by overlapping the edges and applying Butyl tape in between. It is also used to adhere to concrete walls and footings when properly prepared. Butyl Seal is non-hardening and flexible.

Available in 2”x 50’ rolls.

| *These are guidelines only and may not be suitable for all applications. Please Contact Miller Environmental Corp for specific applications. (508-378-3800) | Butyl Seal Tape (MBE2X50TAPE) |
| --- | --- |
| Backing | Coated Release Paper |
| Adhesive | 1 mm Black Butyl Rubber |
| Color | Black |
| Type | Double Sided |
| Size | 2” x 50’ |
| Adhesion Values | 107.5 oz./ inch (to steel) |
| Service Temp. | 30° F to +100° F |
| Minimum Application Temp. | 35° F |
| Ideal Storage Temp./Humidity | 70° F w/ 40-50% Humidity |

Note: To the best of our knowledge, these are typical property values and are intended as guides only, not as specification limits. Miller Environmental Corp. makes no warranties as to the fitness for a specific use or merchantability of products referred to, no guarantee of satisfactory results from reliance upon contained information or recommendations and disclaims all liability for resulting loss or damage.